ALLIED

W-200

Allied W-200 woven geotextile fabrics are woven polypropylene materials offering optimum performance when used in stabilization application. Produced from first quality materials, they provide the perfect balance of strength and separation, functioning exceptionally in a wide range of performance requirements. Allied W-200 meets a AASHTO M288-92 requirements for Class A and Class B Subsurface drainage, Class A and Class B Erosion Control and Medium Survivability Separation Fabrics. Allied W-200 conforms to the physical property values listed below:

| Fabric Property | Test Method | Units | Minimum Average Roll Value |
| --- | --- | --- | --- |
| Weight (Typical) | ASTM D5261 | oz/sq.yd | 4.0 |
| Grab Tensile | ASTM D4632 | Lbs | 200 |
| Grab Elongation | ASTM D4632 | % | 15 (MD) |
| Trapezoidal Tear | ASTM D4533 | Lbs | 75 (MD) |
| Puncture Resistance | ASTM D4833 | Lbs | 90 |
| Mullen Burst | ASTM D3786 | psi | 400 |
| Permittivity | ASTM D4491 | 1/sec | .05 |
| Water Flow (FH) | ASTM D4491 | gpm/sq.ft | 5 |
| AOS | ASTM 4751 | US Seive | 50 |
| UV Resistance (after 500hrs) | ASTM D4355 | % strength retained | 70 |

Roll dimensions:  17.5 ft x 310 ft