ALLIED

NW-12

Allied NW-12 is a superior quality, non-woven geotextile produced by needle punching 100% polypropylene staple fibers in a random network to form a high strength dimensionally stable fabric. The polypropylene is specially formulated to resist ultraviolet light deterioration, and is inert to commonly encountered soil chemicals. The fabric will not rot or mildew, is non-biodegradable, and is resistant to damage from insects and rodents. Allied NW-12 conforms to the physical values listed below.

| Fabric Property | Test Method | Units | Minimum Average Roll Value |
| --- | --- | --- | --- |
| Weight (Typical) | ASTM D5261 | oz/sqyd | 12.0 |
| Grab Tensile | ASTM D4632 | Lbs | 300 |
| Grab Elongation | ASTM D4632 | % | 50 |
| Trapezoidal Tear | ASTM D4533 | Lbs | 115 |
| Puncture Resistance | ASTM D4833 | Lbs | 180 |
| Mullen Burst | ASTM D3786 | Psi | 600 |
| Permittivity | ASTM D4491 | 1/sec | 1 |
| Water Flow (FH) | ASTM D4491 | Gpm/sqft | 75 |
| AOS | ASTM D4751 | Us sieve | 100 |
| UV Resistance (after 500 hrs) | ASTM D4355 | % strength retained | 70 |

Roll dimension:  15 ft x 300 ft.