ALLIED

PROFESSIONAL WEED BARRIER

| FABRIC PROPERTY | WORK INSTRUCTIONS | UNITS | TARGET | MIN | MAX |
| --- | --- | --- | --- | --- | --- |
| Basis Weight (Typical) | LB-WI-GL-102 | oz/sqft | 3.00 | 2.7 | 3.3 |
| MD Grab Tensile | LB-WI-GL-235 | Lbs/in | 59 | 51 | 67 |
| MD Grab Elongation |  | % | 56 | 40 | 72 |
| CD Grab Tensile | LB-WI-GL-235 | Lbs/in | 48.8 | 40.8 | 56.8 |
| CD Grab Elongation |  | % | 87.5 | 65 | 110 |
| MD Trap Tear | LB-WI-GL-139 | Lbs | 30.8 | 21 | 40.6 |
| CD Trap Tear | LB-WI-GL-139 | Lbs | 20.7 | 13 | 28.4 |
| Hunter Color – L** | LB-WI-GL-112 |  | TBD | TBD | TBD |
| Hunter Color – A** | LB-WI-GL-112 |  | TBD | TBD | TBD |
| Hunter Color – B** | LB-WI-GL-112 |  | TBD | TBD | TBD |
| Color |  | Visual | Black | N/A | N/A |

NOTE: 	Allied Professional Weed Barrier requires ground cover to protect it against U.V degradation.

| Packaging |  |
| --- | --- |
| Roll Dimensions – Feet | 6’’ x 300’’ |

**Test once per 12 hour shift.

To the best of our knowledge, the information contained herein as accurate. However, Allied cannot anticipate all conditions under which Allied products or the products of other manufacturers in combination with Allied products, may be used. We accept no responsibility for results obtained by the application of this information of the safety or suitability of our products either alone or in combination with other products. Final determination of the suitability of any information or material for the use contemplated, of its manner of use, and whether the suggested use infringes any patents is the sole responsibility of the user.