ALLIED

Combo Geogrid 31/31

Allied Composite Geogrids are manufactured by a new Geocomposite technology method, superior properties show a structurally sound and stable geogrid. It is especially designed for soil stabilisation and reinforcement applications. The Composite Geogrids are manufactured by bonding ASTM Standard Polyester Geogrid to a nonwoven polymer geotextile.

Specifications

Geogrid Index Properties        Test Method         Units            MD Values        TD Values

Polymer Type				          -			  -		    PET		         -

Minimum Carbon Black		ASTM D 4218            %		      2	                    -

Tensile Strength @ 2% Strain 	ASTM D 6637       KN/m (lb/ft)         12(8,850)	   12(8,850)

Tensile Strength @ 5% Strain	ASTM D 6637       KN/m (lb/ft)         21(15,488)        21(15,488)

Ultimate Tensile Strength		ASTM D 6637       KN/m (lb/ft)         31(22,864)        31(22,864)

Strain @ Ultimate Strength		ASTM D 6637            %  	                13	                   13

Geotextile Physical Properties									____

Mass per Unit Area			ASTM D 5261     g/m2 (oz/sq.yd)      300(8.85) 	         -

Color					          -		              -	              White	         -

Opening Size				ASTM D 4751            mm	               0.07		         -

Durability												____

UV Resistance			EN ISO 12224	  %		     95		         -

Dimensions												____

Roll Width				        -		           m (ft)	           3.9(12.8)	         -

Roll Length				        -		           m (ft)	            50(164)	         -

Roll Area				        -		       sq.m(sq.ft)         195(2099)	         -