SECTION 07 18 16

MasterSeal® Traffic 2500 Deck Coating System

(Formerly Conipur II Deck Coating System)

NoteS to specifiers:

The Construction Systems business of BASF Corporation previously conducted business as Degussa, Inc. Building Systems.  The Admixture Systems business of BASF Corporation previously conducted business as Degussa Admixtures, Inc. and Master Builders, Inc.

On January 1, 2014 BASF launched the Master Builders Solutions brand in North America. With Master Builders Solutions, BASF combined its existing construction brands such as Master Builders, Chemrex, Sonneborn, MBT and others that have established a legacy of innovation, to create one unparalleled, globally recognized brand for its solutions to the construction industry.

This new BASF harmonized naming system, presents simpler, more logical and easier to understand product names. Each new name reflects an application property or function.

The purpose of this guide specification is to assist the specifier in developing a project specification for the use of BASF’s roducts.  it is not intended to be a “stand alone” document, nor to be copied directly into a project manual.  This guide specification will need to be carefully reviewed for APPROPRIATENESS for the given project and edited accordingly to comply with project-specific requirements.

- GENERAL

      - SUMMARY

        - Section Includes:

          - Application of high-solids, fluid-applied, polyurethane, waterproofing, traffic-bearing, membrane deck coating system.

edit note:  Delete sections below not relevant to this project; add others as required.

        - Related Sections:

          - Section 03 30 00 - Cast-in-Place Concrete.

      - SUBMITTALS

        - Comply with Section [01 33 00] [__ __ __].

        - Product Data:  Submit manufacturer's technical data sheets and LEED product information for each product.

        - Submit list of project references as documented in this Specification under Quality Assurance Article.  Include contact name and phone number of person charged with oversight of each project.

        - Quality Control Submittals:

          - Provide protection plan of surrounding areas and non-work surfaces.

      - QUALITY ASSURANCE

        - Comply with Section [01 40 00] [__ __ __].

        - Qualifications:

          - Manufacturer Qualifications:  Company with minimum 15 years of experience in manufacturing of specified products and system.

          - Manufacturer Qualifications:  Company shall be ISO 9001:2000 Certified.

          - Applicator Qualifications:  Company with minimum of 5 years experience in application of specified products and system on projects of similar size and scope, and is acceptable to product manufacturer.

            - Successful completion of a minimum of 5 projects of similar size and complexity to specified Work.

        - Field Sample:

          - Install at Project site or pre-selected area of building an area for field sample, as directed by Architect.

          - Provide mock-up of at least 100 square feet (9.3 m2) to include surface profile, sealant joint, crack, flashing, and juncture details and allow for evaluation of slip resistance and appearance.

          - Apply material in accordance with manufacturer’s written application instructions.

          - Manufacturer’s representative or designated representative will review technical aspects; surface preparation, application, and workmanship.

          - Field sample will be standard for judging workmanship on remainder of Project.

          - Maintain field sample during construction for workmanship comparison.

          - Do not alter, move, or destroy field sample until Work is completed and approved by Architect.

          - Obtain Architect’s written approval of field sample before start of material application, including approval of aesthetics, color, texture, and appearance.

      - DELIVERY, STORAGE, AND HANDLING

        - Comply with Section [01 60 00] [__ __ __].

        - Comply with manufacturer’s ordering instructions and lead-time requirements to avoid construction delays.

        - Deliver materials in manufacturer's original, unopened, undamaged containers with identification labels intact.

        - Store materials in unopened packaging in clean, dry area protected from sunlight.

      - PROJECT CONDITIONS

        - Environmental Requirements:

          - Minimum Application Temperature:  40 degrees F (4 degrees C).

          - Do not apply in rain or when rain is expected within 24 hours.

          - Do not apply above 90 degrees F (32 degrees C).

- PRODUCTS

      - MANUFACTURERs

        - Subject to compliance with requirements, provide products from the following manufacturer:

BASF Corporation

Construction Chemicals

889 Valley Park Drive

Shakopee, MN  55379

Customer Service:  800-433-9517

Technical Service:  800-243-6739

Direct Phone:  952-496-6000

Internet: www.master-builders-solutions.basf.us

        - Substitutions:  Comply with Section [01 60 00] [__ __ __].

        - Specifications and Drawings are based on manufacturer's proprietary literature from BASF Construction Chemicals.  Other manufacturers shall comply with minimum levels of material, color selection, and detailing indicated in Specifications or on Drawings.  Architect will be sole judge of appropriateness of substitutions.

      - MATERIALS

        - High-solids, fluid-applied, polyurethane, waterproofing, traffic-bearing, membrane deck coating system.

          - Acceptable Product:  MasterSeal Traffic 2500 Deck Coating System (formerly Conipur II Deck Coating System) by BASF.

            - Primer:  MasterSeal P 255 (formerly Conipur 78 Primer.)  2-component, polyurethane-based adhesive primer.

            - Base coat:  MasterSeal M 265 (formerly Conipur 265-Z Base Coat.)  2-component, fast-curing, polyurethane base coat.

edit note:  Delete top coat not required.

            - Top Coat:  MasterSeal TC 275 (formerly Conipur 275 Top Coat):  2-component, fast-curing, aromatic polyurethane top coat.

            - Aliphatic Top Coat:  MasterSeal TC 295 (formerly Conipur 295 Top Coat):  2-component, aliphatic, 100 percent solids, polyurethane, waterproofing top coat.

        - Performance Requirements:  Provide materials complying with the following requirements:

          - Crack Bridging, Base Coat, ASTM C957:  Passes.

          - Adhesion Peel, Primer and Base Coat, ASTM C957.

            - Plywood:  25 pli.

            - Concrete:  14 pli.

          - Tensile Strength, ASTM D412:

            - Base Coat:  2,500 psi (17.2 MPa).

            - Top Coat:  3,000 psi (20.7 MPa).

            - Aliphatic Top Coat:  2,980 psi (20.6 MPa).

          - Elongation, ASTM D412:

            - Base Coat:  900 percent.

            - Top Coat:  30 percent.

            - Aliphatic Top Coat:  375 percent.

          - Hardness, ASTM D2240, Shore D:

            - Top Coat:  70.

            - Aliphatic Top Coat:  45.

          - Taber Abrasion Resistance, ASTM D4060, CS-17 Wheel, 1,000 g load, 1,000 cycles:

            - Primer/Base Coat/Top Coat:  100 mg.

            - Primer/Base Coat/Intermediate Top Coat/Aliphatic Top Coat:  58 mg.

          - Solids Content:

            - Primer:  99 percent.

            - Base Coat:  99 percent.

            - Top Coat:  99 percent.

            - Aliphatic Top Coat:  99 percent.

          - VOC Content:

            - Primer:

              - Part A:  0.08 lbs per gal (10 g/L), less water and exempt solvents, when components are mixed.

              - Part B:  0.08 lbs per gal (10 g/L), less water and exempt solvents, when components are mixed.

            - Base Coat:

              - Part A:  0.03 lbs per gal (4 g/L), less water and exempt solvents, when components are mixed.

              - Part B:  0.04 lbs per gal (5 g/L), less water and exempt solvents, when components are mixed.

            - Top Coat:

              - Part A:  0.59 lbs per gal (71 g/L), less water and exempt solvents, when components are mixed.

              - Part B:  0.11 lbs per gal (13 g/L), less water and exempt solvents, when components are mixed.

            - Aliphatic Top Coat:

              - Part A:  0 lbs per gal (0 g/L), less water and exempt solvents, when components are mixed.

              - Part B:  0.04 lbs per gal (5 g/L), less water and exempt solvents, when components are mixed.

        - Color:

edit note:  delete colors not required.

          - Black.

          - Charcoal.

          - Gray.

        - Accessories:

          - Aggregate:  MasterSeal 941 (formerly Sonoguard Aggregate).

          - Sealant Primer:  MasterSeal P 173 (formerly Sonneborn Primer 733).

          - Sealant:  MasterSeal SL 2 or MasterSeal CR 195 (formerly Sonneborn SL-2 or Sonneborn Ultra).

          - Deep Joint Sealant:  MasterSeal SL 2 or MasterSeal NP 2 (formerly Sonneborn SL-2 or Sonneborn NP-2).

          - Plywood Joint Sealant:  MasterSeal NP 1 or MasterSeal NP 2 (formerly Sonneborn NP-1 or Sonneborn NP-2).

          - Reinforcing Fabric:  MasterSeal 995 (formerly Sonoshield Reinforcing Fabric).

- eXECUTION

      - EXAMINATION

        - Comply with Section [01 70 00] [__ __ __].

      - SURFACE PREPARATION

        - Protection:  Protect adjacent Work areas and finish surfaces from damage during deck coating system application.

        - Prepare surface in accordance with manufacturer’s instructions.

edit note:  delete if concrete substrate not present.

        - Concrete:

          - Minimum Compressive Strength:  3,000 psi (21 MPa).

          - Cure concrete for a minimum of 28 days.

          - Ensure concrete is structurally sound, clean, and dry in accordance with ASTM D4263.

          - Repair voids and delaminated areas.

          - Shotblast concrete to remove dirt, dust, grease, oil, coatings, laitance, and other surface contamination and to provide profile for proper adhesion.

          - Profile:  Minimum of ICRI CSP-3 (approximately 80 to 100-grit sandpaper).

          - Prestripe and prepare cracks, joints, and detail work in accordance with manufacturer’s instructions.

edit note:  delete if metal substrate not present.

        - Metal:

          - Remove dust, debris, and other contaminants from vent, drain pipe, and post penetrations; reglets; and other metal surfaces.

          - Clean surfaces to bright metal and prime immediately with sealant primer.

          - Provide appropriate cant with deep joint sealant to eliminate 90-degree angles.

edit note:  delete if plywood substrate not present.

        - Plywood:

          - Smooth-faced, APA-stamped, and exterior grade.  Conform to code, with plywood not less than 15/32 inch (12 mm) thick.  Follow APA guidelines for plywood spacing and deck construction.

          - Ensure surfaces free of contaminants.

          - Caulk seams with plywood joint sealants.  Prestripe 4 to 6 inches (102 to 152 mm) wide with 25 wet mils (0.6 mm) of base coat.  Reinforce seams between plywood sheets and between flashing and plywood deck by embedding reinforcing fabric into prestriping.

          - Provide appropriate cant with deep joint sealant to eliminate 90-degree angles.

      - mixing

        - Mix material components in accordance with manufacturer’s instructions.

        - Precondition material components to a temperature of 70 degrees F (21 degrees C) before mixing.

      - application – GENERAL

        - Apply deck coating system in accordance with manufacturer’s instructions.

        - Do not apply deck coating system to damp, wet, or contaminated surfaces.

edit note:  Select systems as required.  delete systems not required. MasterSeal Traffic 2500 Deck coating system can be applied using several methods, depending upon the degree of traffic to which the system will be exposed.

      - APPLICATION – LIGHT TRAFFIC AND PARKING STALLS

        - Primer:  Apply 4 wet mils (0.1 mm).

        - Base Coat:  Apply 25 wet mils (0.5 mm).  Allow base coat to cure 3 to 4 hours.

        - Top Coat:  Apply 20 wet mils (0.5 mm).

        - Aggregate:  Immediately broadcast aggregate at rate of 10 to 15 lbs per 100 sq ft (0.5 to 0.75 kg/m2) into wet top coat.  Backroll to encapsulate.

      - APPLICATION – MEDIUM TRAFFIC

        - Primer:  Apply 4 wet mils (0.1 mm).

        - Base Coat:  Apply 25 wet mils (0.5 mm).  Allow base coat to cure 3 to 4 hours.

        - Intermediate Coat:  Apply 15 wet mils (0.4 mm).  Immediately backroll to level material.

        - Aggregate:  Immediately broadcast aggregate to refusal into wet intermediate coat.  Allow curing time of 3 to 4 hours.

        - Top Coat:  Apply 12 to 15 wet mils (0.3 to 0.4 mm).  Immediately backroll to level material.

        - Aggregate:  Immediately broadcast aggregate at rate of 3 to 5 lbs per 100 sq ft (0.15 to 0.25 kg/m2) into wet top coat.  Lightly backroll to encapsulate.

      - APPLICATION – EXTRA-HEAVY TRAFFIC

        - Primer:  Apply 4 wet mils (0.1 mm).

        - Base Coat:  Apply 25 wet mils (0.5 mm).  Immediately backroll to level material.  Allow base coat to cure 3 to 4 hours.

        - Intermediate Coat:  Apply 20 to 25 wet mils (0.5 to 0.6 mm).  Immediately backroll to level material.

        - Aggregate:  Immediately broadcast aggregate to refusal into wet intermediate coat.  Allow curing time of 3 to 4 hours.

        - Remove excess aggregate.

        - Top Coat:  Apply 15 wet mils (0.40 mm).  Immediately backroll to level material.

        - Additional Slip Resistance:  Immediately broadcast aggregate at rate of 3 to 5 lbs per 100 sq ft (0.15 to 0.25 kg/m2).  Lightly backroll into top coat.

      - PROTECTION

        - Pedestrian Traffic:  Allow minimum curing time of 4 hours before allowing pedestrian traffic onto deck coating system.

        - Vehicular Traffic:  Allow minimum curing time of 24 hours before allowing vehicular traffic onto deck coating system.

        - Protect completed deck coating system from damage and staining during construction.

END OF SECTION

Disclaimer

This information and all further technical advice are based on BASF’s present knowledge and experience. However, BASF assumes no liability for providing such information and advice including the extent to which such information and advice may relate to existing third party intellectual property rights, especially patent rights. In particular, BASF disclaims all CONDITIONS AND WARRANTIES, WHETHER EXPRESS OR IMPLIED, INCLUDING THE IMPLIED WARRANTIES OF FITNESS FOR A PARTICULAR PURPOSE OR MERCHANTABILITY. BASF SHALL NOT BE RESPONSIBLE FOR CONSEQUENTIAL, INDIRECT OR INCIDENTAL DAMAGES (INCLUDING LOSS OF PROFITS) OF ANY KIND. BASF reserves the right to make any changes according to technological progress or further developments. It is the customer’s responsibility and obligation to carefully inspect and test any incoming goods. Performance of the product(s) described herein should be verified by testing and carried out only by qualified experts. It is the sole responsibility of the customer to carry out and arrange for any such testing. Reference to trade names used by other companies is neither a recommendation, nor an endorsement of any product and does not imply that similar products could not be used.