ALLIED

AC 30 VOC

SILOXANE SEALER

USES

AC 30 VOC had been primarily designed to seal concrete slabs / decks / walls / abutments from both water and chloride intrusion while providing for water vapour transmission (breathability). AC 30 VOC will provide similar protection to cement-based masonry and stucco surfaces, inhibiting the penetration of most water-borne atmospheric pollutants.

ADVANTAGES

- Markedly reduces water and chloride intrusion.

- Prevents staining and discoloration due to electro-static attraction of dust particles.

- Increases freeze thaw resistance.

- Inhibits efflorescence.

- Breathable system provides for water vapour transmission.

- UV resistant – will not yellow.

- Can be applied to damp surfaces.

- Deep penetration into substrate.

- Non-film forming – does not alter surface texture or skid-resistance.

DESCRIPTION

AC 30 VOC is an oligomeric alkoxy-siloxane which penetrates concrete or Portland cement based stucco or mortar and chemically bonds within the substrate by reacting with free silica and moisture either present in the substrate or in the atmosphere. The highly hydrophobic chemical molecules are extremely small resulting in penetration depths up to 5mm. AC 30 VOC as a penetrant is not film forming and will not significantly change the appearance or slip-resistance of the substrate. It may slightly darken the surface to which it is applied.

PROPERTIES

Water Absorption (actual test results).

PERCENT WATER ABSORPTION

Masonry Material	   Exposure Hours      Control (Untreated)	       Treated with AC 30

Concrete Brick *		   48			  7.28			        0.53

50mm Cement Mortar*

Cubes per SS-W-11ob		   72			   8.0			        0.48

*Immersed in AC 30 VOC for 5 seconds and then air dried for 24 hours, weighted and placed in a pan containing a constant level of ¼’’ of water. After 48 hours in the pan of water, they were removed, wiped free of excess surface moisture, and reweighted.

OVER

INSTRUCTIONS FOR USE

The substrate should be structurally sound and free of grease, oil, sealers, coating, or other surface contaminants. Broom finish, swirl trowel finish or lightly brush blasted concrete surfaces lend themselves to penetration of AC 30 VOC. Tightly troweled concrete finishes will not allow proper penetration of the sealer. New concrete should be wet cured for 28 days before application of AC 30 VOC. Do not use liquid applied curing compounds and concrete pores will become clogged preventing penetration of AC 30. (Consider using Allied Micro-Perf Concrete Curing Blanket) AC 30 VOC may be applied to slightly damp surfaces, providing no free water exists. Apply full flood coat evenly over the surface by roller or sprayer. Very hot dry concrete may be fogged with water prior to sealer application to cool the surface. Allow any very wet areas to surface-dry before applying AC 30 VOC. After 10 minutes of penetration pick up any puddled AC 30 VOC remaining on the surface with a dry roller, rag, or mop to avoid non-uniform coloration. Apply to vertical surfaces in two coats one immediately after the other.

LIMITATIONS

AC 30 VOC is designed to resist penetration of water-borne chlorides. Solvent and oil-based products will penetrate and stain concrete sealed with AC 30 VOC. Solvent-carried acrylic and methacrylate topcoats may be applied over AC 30 VOC if resistance to oil staining is desired. AC 30 VOC cannot compensate for substandard concrete mix designs for finishing techniques. It can only enhance the performance of good concrete. Durable concrete will have a low water-cement ratio, adequate air entrainment and high strength. Consult your concrete producer for recommendations.

PRECAUTIONS

AC 30 VOC will slightly darken the surface appearance of the substrate to which it is applied. All control joint, crack, and expansion joint sealing should be completed prior to application of AC 30 VOC. Do not apply in direct sunlight when temperature is over 32°C (90°F). Cooler temperatures will slow down the evaporation of VOC compliant solvents and improve penetration of AC 30 VOC. Do not apply when air or surface temperature if below 4°C (39°F).

HEALTH and SAFETY

Avoid prolonged or repeated contact with skin. In case of skin contact, flush with plenty of water. For eyes, immediately flush with plenty of water for 15 minutes and obtain medical attention. Avoid prolonged breathing of vapour or spray mist. If affected by inhalation of vapour, remove to fresh air. If swallowed, call a physician immediately. DO NOT INDUCE VOMITING. Review MSDS for complete information. FIRE: Keep away from heat and flame. Use only with adequate ventilation. FOR INDUSTRIAL USE ONLY – KEEP OUT OF REACH OF CHILDREN.

COVERAGE

Recommended coverage rates: 3.5 – 5.0 sqm/litre		(175 – 245 sq.ft/gal)

VOC CONTENT: 246 g/litre

Compliant Solvent

PACKAGING

AC 30 is supplied in 4 litre cans, 17 litre pails and 205 litre drums.